Vol. xx (Nomor), Year, page.

DOI :

# The Effect of Sintering Temperature on Hydrophobic Characteristic of Silica Manganese /Polystyrene (SiMn/PS) Nanocomposite

# Dian Septiana 1, Ratnawulan*2

1 Department of Physics,Padang State University, Jalan Prof. Dr Hamka, Air Tawar Barat, Padang, West Sumatra, 25171. Indonesia

Corresponding author. Email: dianseptiana527@gmail.com & ratnawulan320@fmipa.unp.ac.id

ABSTRACT

Currently a lot of research has been done on hydrophobic layers, but in its application the layer is easily damaged and is not corrosion resistant. Therefore, this research intends to decide the effect of variations in sintering temperature on the hydrophobic characteristic of SiMn/PS nanocomposite layers using a sintering temperature of 60oC, 100oC, 140oC, 180oC and 200oC for 1 hour using a furnace. This research was conducted in the Material Physics Laboratory of0the Faculty of0Mathematics and Natural Sciences and the Chemistry Laboratory of0the Faculty of0Mathematics and Natural Sciences, Padang State University.This research uses HEM-3D (High Energy Milling Ellipse-3D Mention), XRD (X-Ray Difraction) and0SEM (Scanning Electron Microscope) tools. The precursor was made by giving 0.5 grams of polystyrene, 0.2 grams of silica powder and 0.2 grams of manganese powder. Coating is done by spin coating method. The results of this research from the variation of the sintering temperature showed that the SiMn/PS nanocomposite layer was hydrophobic based on the contact angle test. The highest contact angle is at a temperature of 600C.

Keywords : hydrophobic, contact angle, durability, nanocomposite, polystyrene, Silica Oxide (SiO2), Manganese (Mn).

This is an open access article distributed under the Creative Commons 4.0 Attribution License, which permits unrestricted use, distribution, and reproduction in any medium, provided the original work is properly cited. © 2019 by author and Universitas Negeri Padang.

- INTRODUCTION

With the development of this era, there have been many research to create a hydrophobic surface. However, in use, the layer is easily damaged and easily corroded due to contact with other objects. Therefore, the development of a strong and durable hydrophobic layer and corrosion resistance with an easy and efficient method is very necessary.

Hydrophobic can be defined as water-repellent properties, has a large contact angle of 900C and an unpleasant surface. A surface can be said to be hydrophobic if it has certain characteristics. Surface characteristics that are hydrophobic include having anti-wet properties, always looking clean, having a large contact angle of 900C [4]. The hydrophobicity of a surface can be dictated by estimating the contact angel shaped between the water and the sample surface [3].Surfaces that are hydrophobic have a contact angle between 90°- 150°, while a surface that has a contact angle of >150° is called superhydrophobic [7].

The substrates used are those that have not corrosion characteristic such as manganese and strong characteristic such as silica which are made into nanocomposites. Nanocomposite is a combination of two or more materials consisting of a matrix and a reinforcement measuring 1.0 x 10-9 m. Silica is a metal oxide compound that is widely found in nature, but its presence is not free but is bound to other compounds both physically and chemically[5]. The three predominant crystalline phases of silica are quartz, tridymite, and crystobalite[12]. The course of action of particles in shapeless silica happens haphazardly with a low level of regularity. Therefore, it is necessary to carry out a silica sand purification process to remove impurities. Manganese is one of the most abundant elements found in the earth's crust which has a gray black color.

For the manufacture of the coating required a polymer, the polymer used is polystyrene. This polystyrene is resistant to acids, bases and other rusting agents. Many methods are used for this purpose, such as electrochemical reactions,phase separation, sin coating, dip coating, sol-gel, coprecipitation and fillingparticles [11]. The method used to create layers SiMn/PS nanocomposite is spin-coating. Relative spin-coating methodeasy to use, homogeneous coating, and not very expensive.

Temperature sintering is a heating process at a high temperature in any case, beneath the dissolving point until a change in the microstructure occurs. Giving this temperature variation to see a change in the contact angle [9] and the morphology of the layers[6]. There is treatment heat causes bonding between powder particles and increases thestrength of the resulting product [2].

## METHOD

This research is an experimental research type. This study examines the effect of variations in the sintering temperature of SiMn/PS nanocomposite on the hydrophobic characteristic. This research was directed at the Material Physics and Biophysics Laboratory of0the Faculty of0Mathematics and Natural Sciences and the Chemistry Laboratory of the State University of Padang. The materials used are nanoparticles of silica, manganese, polystyrene (PS), tetrahydrofuran (THF) and aquadest. The tools used are measuring cups, beakers,

magnetic stirrer, glass (size 0.5 cm x 0.5 cm and 1 cm x 1cm), camera, XRD, FTIR, HEM, furnace, oven and spin coating.

There are several steps that are carried out:

- Sample Preparation Stage

  - Synthesis of silica and manganese nanoparticles

Weighing 8 grams of silica and manganese each for grinding using HEM-E3D. Grinding silica with HEM-E3D for 5 hours. Grind manganese with HEM-E3D for 16 hours.

  - Stages of making Silica Manganese/Polystyrene precursor

Dissolve 0.5 grams polystyrene and 15 ml tetrahydrofuran using a magnetic stirrer with temperature 500C. Then mix 0.2 grams of silica powder and 0.2 grams of manganese with polystyrene solution, stirred for 1 hour using a magnetic stirrer until homogeneous.

  - Sample preparation stage

Cut the glass slides with sizes of 0.5 cm x 0.5 cm and 1cm x 1cm then wash them using an ultrasonic cleaner by immersing the glass in PEG and aquadest solution for 2 hours.

  - The stage of making a thin layer using spin coating

Putting the glass substrate to be coated onto a spin coater, then instilling a silica manganese/polystyrene (SiMn/PS) nanocomposite solution with a dropper in 60 seconds with a rotating speed of 500rpm.

  - The sample heating stage using a furnace

Manganese silica naocomposite layer formed in the furnace with temperature variations of 60oC, 100oC, 140oC, 180oC and 200oC for 1 hour.Heating the sample is done by entering the sample into the furnace and the sintering temperature is set for 1 hour.

  - Contact angle measurement stage

Taking photos for contact angles using a camera in a dark room. Then to measure the contact angle using ImageJ software. Here's how the ImageJ software looks and works.

Fig.1.ImageJ Software Display

To measure the contact angle, select the image to be measured in the file tool, after the image appears then select the angle tool and then draw a straight line between the surface and the water droplet and draw the line up until it forms an angle between the sample surface and the droplet.

Fig.2. Measuring Contact Angle

To find out the contact angle, select Analyze then select Maesure and the results of the contact angle will be displayed. After making repeated measurements and then looking for the average.

- Analysis Stage

The contact angle analysis obtained from the measurement results of the SilicaManganese/Polystyrene (SiMn/PS) nanocomposite layer can be calculated by the following formula:

Contact angle =𝑟igh𝑡 𝑐𝑜𝑛𝑡𝑎𝑐𝑡 𝑎𝑛g𝑒𝑙+ 𝑙𝑒ƒ𝑡 𝑐𝑜𝑛𝑡𝑎𝑐𝑡 𝑎𝑛g𝑒𝑙

2

(1)

Then the resulting data is described in the form of a graph. The effect of temperature on the contact angle can be determined by plotting the data on the X and Y coordinates using the Microsoft Excel program.

## RESULTS AND DISCUSSION

The results of this research consist of identification of contact angle taken from measurements on a thin layer of Silica Manganese/Polystyrene (SiMn/PS) nanocomposite with sintering temperatures of 60oC, 100oC, 140oC, 180oC and 200oC which have been tested using Image-J software.

- SiMn/PS coating contact angle temperature 60oC

Fig.3. Contact Angle from a Temperature of 60oC

Table 1. Results of contact angel from a temperature of 60oC

Contact Angel Measurement Results

The Calculation Results

θ Right	θ Left	θ

104,986o	105,457o	105,221o

104,484o	104,339o	104,411o

105,287o	105,097o	105,197o

104,706o	104,925o	104,817o

104,321o	103,389o	103,855o

Average	104.7o

- SiMn/PS coating contact angle temperature100oC

Fig.4. Contact Angle from a Temperature of

100oC

Table 2. Results of contact angel from a temperature of 100oC

Contact Angel Measurement Results

The Calculation Results

θ Right	θ Left	θ

95,229o	94,251o	95.74o

95,805o	95,744o	95,774o

96,881o	95,756o	96,318o

95,036o	95,541o	95,288o

95,200o	95,537o	95,368o

Average	95,497 o

- SiMn/PS coating contact angle temperature140oC

Fig.5. Contact Angle from a Temperature of

140oC

Table 3. Results of contact angel from a temperature of 140oC

Contact Angel

Measurement Results

The Calculation Results

θ Right	θ Left	θ

92,245o	93,072o	92,658o

92,726o	92,513o	92,637o

92,984o	92,441o	92,712o

92.821o	92,122o	92,472o

92,153o	92,214o	92,183o

Average	92,523o

- SiMn/PS coating contact angle temperature180oC

Fig.6. Contact Angle from a Temperature of 180oC

Table 4. Results of contact angel from a temperature of 180oC

Contact Angel Measurement Results

The Calculation Results

θ Right	θ Left	θ

90,300o	90,515o	90,407o

90,000o	90,175o	90,087o

90,384o	90,000o	90,192o

90,212o	90,395o	90.303o

90,124o	90,184o	90,154o

Average	90,228o

- SiMn/PS coating contact angle temperature200oC

Fig.7. Contact Angle from a Temperature of

200oC

Table 5. Results of contact angel from a temperature of 200oC

Contact Angel

Measurement Results

The Calculation Results

θ Right	θ Left	θ

82,593o	83,202 o	82,897o

82,638o	82,110 o	82.37o

82,143o	83,018 o	82,580o

82,544o	82,532 o	82,538o

82,314o	82,143 o	82,228o

Average	82,522o

105

100

Sudut Kontak (0)

95

90

85

80

20  40   60   80  100   120    140    160    180    200    220

Temperatur Sintering (0C)

Fig.8. Relationship between Sintering Temperature and Contact Angle Measurement

.

From the graph it can be seen that the sintering temperature greatly affects the resulting contact angle. The highest contact angle is obtained at temperature 60oC by 104.7o In this condition the layers are hydrophobic. However, at a temperature of 200oC the resulting contact angle is 82,522o. This is because the polystyrene polymer contained in the sample layer has melted. Therefore, in this condition the coating is no longer hydrophobic but hydrophilic.

220

200

180

160

%Transmitansi

140

120

100

80

60

40

20

0

3379.11 cm-1

1639.75 cm-1

919.32 cm-1

538.42 cm-1

767.56 cm-1

100

90

80

70

%Transmitansi

60

50

40

30

20

10

0

3365.13cm-1

1641.11 cm-1

540.51 cm-1

767.69 cm-1

919.53 cm-1

4000   3500   3000   2500   2000   1500   1000	500

cm-1

4000  3500   3000   2500   2000   1500   1000    500

cm-1

(a)	(b)

3742.71 cm-1

1031.53 cm-1

540.34 cm

2917.81 cm-1

130

125

120

115

% Transmitansi

110

105

100

95	-1

90

85

80

75

70

4000	3500	3000	2500	2000	1500	1000	500

cm-1

# (c )

140

3742.84 cm-1

163329 cm-1

541.12 cm

3376.48 cm-1

130

%Transmitansi

120

110	-1

100

90

80

70

4000	3500	3000	2500	2000	1500	1000	500

cm-1

# (d)

220

200

180

-1

160

540.03 cm

140

-1

3742.46 cm

-1

1453.49 cm

2937.25 cm

-1

-1

120

1725.79 cm 1153.31 cm-1

100

80

%Transmitansi

4000	3500	3000	2500	2000	1500	1000	500

cm-1

(e)

Fig.9. (a) Results of FTIR from a temperature of 60oC (b) Results of FTIR from a temperature of 100oC (c) Results of FTIR from a temperature of 140oC (d) Results of FTIR from a temperature of 180oC (e) Results of FTIR from a temperature of 200oC

The desired groups are Si-O, Mn-O, C=C and C-H which indicate the presence of polystyrene. The absorption peak in the wave number region of 540.51 cm-1 comes from the Mn-O bond stretch (MO: 400-560 cm-1) [8], 767.69 cm-1 comes from the Si-O stretch with a range of 782 - 805 cm-1[1], while for the functional group of polystyrene there are C=C and CH groups and it can be seen that C=C with wave numbers 1641.11 cm-1 and CH wave numbers 919.53 cm-1 and 2917.81 cm-1 (CH: 750 cm- 1 - 2937 cm-1) [10]. From the data above which shows that the group is present at a sintering temperature of 60oC and 1000C.

## CONCLUSION

Based on the research that has been carried out, it very well may be reasoned that the SiMn/PS nanocomposite layer is hydrophobic at a sintering temperature of 600C-1800C and the highest contact angle at a temperature of 600C. At a temperature of 2000C layer character hydrophilic.

## ACKNOWLEDGMENT

Thanks to Dr. Ratnawulan, M.Si who has guided this research to completion.

## REFERENCES

- Apriliya, Gita Ayu. 2015. Karakterisasi Termomekani Komposit PED 4000/Silika Amorf Menggunakan Dynamic Mechanical Analysis (DMA). Tugas Akhir.   Surabaya:   Institut Teknologi Sepuluh Nopember Jurusan Fisika.

- Darvina, Y., & Desnita, D.2019. Pengaruh Suhu Sintering Terhadap Sifat Penyerapan Gelombang Mikro dari Nanokomposit Cofe2o4/PVDF0yang di Preparasi Dengan Metode Sol-Gel. PILLAR OP PHYSICS 12(12).

- Ensikat, Hans J,   dkk. 2011.   Superhydrophobicity in perfection the outstandin   properties of the lotus leaf. Beilstein  Journal of Nanotechnology. Hal 152-161.

- Feng, Lin,dkk. 20202. Super-Hydrophobic Surface From Natural To Atifical Advanced Materials. Vol14, No. 24, Desember 2002.

- Hildayati, dkk 2009. Sintesi dan Karakterisasi Bahan Komposit Karet Alam Silika. ITS Surabaya.

- Irawati, A.F, Zainuri, M. 2016. Pengaruh Temperature Perlakuan   Panas   Pada Lapisan Hydrophobic Komposit PDMS/SiO2 Dengan Fasa Silika Kristobalit. Jurnal sains dan Seni ITS Vol. 5, No.1, (2016) 2337-3520

- Karthick,	B dan Ramesh Maheshwari,	2008.	Lotus-Inspired Nanotechnology Applications. Resonance, General Article.

- Nakamoto,	K.	1986.	Infrared and0Raman Spectra of0Inorganic and0Coordination Compound 4th edition. New York:John Wiley and Sons  Inc.

- Rohmah, R. 2016. Pengaruh Variasi Temperatur Kalsinasi Sio2 Terhadap Sifat Kebasahan Pada Permukaan Hidrofobik (Doctoral dissertation, Institut Teknologi Sepuluh Nopember Surabaya).

- Sembiring, S., & Simanjutak, W. 2019. Karakteristik fungsional dan sifat fisis aspal akibat penambahan silika sekam padi. Jurnal Teori dan Aplikasi Fisika, 7(01), 77-82.

- Setiawati, T., Amalia, I. S., Sulistiso,   G   S., & Wisnu, A. A. 2019. Sintesis Lapisan Tipis TiO2 dan Analisis Sifat Fotokatalisnya. Jurnal sains materi Indonesia, 141-146.

- Szostak R. 1998. Mollecular  Sieves: Principles of Synthesis and Identification. Springer.